# Solar shading system – DUCO Ventilation & Sun Control DucoSun 95C Verticaal

## Description

DucoSun 95C is an architectural component system with fixed "C" louvres. Thanks to the patented DUCO “Slide-Click” system, the louvre blades are secured quickly and easily in a fixed

## Version

* Shape of blade 95C
* Blade height 71 mm
* Blade depth 71 mm
* Blade angle 45°
* Pitch 122,5 mm
* Blade length Maximum 6000 mm
* Installation depth

|  |  |
| --- | --- |
| **Mullion** | **Installation depth** |
| **50/12** | 91 mm |
| **21/50 Multi** | 129 mm |
| **30/50** | 129 mm |
| **50/50** | 129 mm |
| **42/62** | 141 mm |
| **42/72** | 150 mm |
| **50/125** | 204 mm |

## Material and surface treatment

### Blades and mullions

* Aluminium EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 1,3 mm

* Finish
  + Natural anodised (15-20 μm) according to Qualanod
  + Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Clips

* Plastic Polyamide PA 6.6 – glass fibre reinforced